GRYPHIN COMPANY, INC.

DURADECK SERIES

Non-Skid Coatings

G-2216 	Heavy-duty Epoxy Non-Skid Coating

G-501 	Lightweight Epoxy Non-Skid Coating

G-501-MI-7 	Lightweight Epoxy Non-Skid, Static-Eliminating Coating

G-1191 	One-Part Water-Based Non-Skid Coating

# GENERAL DESCRIPTION

Gryphin G-2216 Non-Skid is a two-component, heavy-duty epoxy non-skid coating containing a synthetic resinous binder system and abrasive particles. This material was designed for use over Gryphin G-249 Epoxy Primer or Gryphin G-250 Chelating Primer. This system can be used on steel, aluminum or concrete when a heavy-duty non-skid is required. G-2216 Non-Skid features excellent resistance to oils, grease, hydraulic fluids, detergent solutions, salt water, alcohol, gasoline, and most acids. Because of its excellent resistance to wear and extreme temperature changes, G-2216 Epoxy Non-Skid will provide years of service if properly applied.

This coating meets the performance requirement of MIL-D-23003 (S), MIL-D-24483A(S) and DOD-C-24667.

USES: Warehouse floors, parking garages, walkways, railroad cars, factory work areas, loading ramps, and any surfaces needing non-skid properties.

# SURFACE PREPARATION

As with any coating application, the better the preparation, the better the results. Prior to coating application, the surface must be clean, dry, and free of oil, grease, and other contaminants. Recommended for steel: 3 mil profile or near-white metal. The procedure to be followed in surface preparation is as follows:

# Clear the area to be cleaned of all loose equipment and rolling stock.

# Rope off an area of convenient size for cleaning and priming.

# Post "Keep Off' and "No Smoking" signs.

# For metal surfaces:

# Clean the area with a Tenant Machine followed by sanding with disc or drum sander

b.  Remove all dust with dry oil-free compressed air.

c. Coat the surface with Gryphin G-249 or G-250 Primer.

5. For concrete surfaces:

a. Sandblast with dry, grease-free sand.

- If sandblasting is not possible, clean with Tenant Machine followed by disc     sander.

- Remove all dust with dry oil-free compressed air.

d. Coat the surface with Gryphin G-249 or G-250 Primer.

6. For more detailed instructions, see Gryphin Bulletin for Surface Preparation.

# APPLICATION METHOD

G-2216 Epoxy Non-Skid can be applied by rolling, spraying, brushing or trowelling.

MIXING INSTRUCTIONS

G-2216 Epoxy Non-Skid is a two-part deck covering compound. The two parts must be thoroughly mixed before use. The following procedure is recommended:

# If G-2216 Epoxy Non-Skid has been stored in the sun, it is recommended that it be placed under cover for 24 hours before mixing. This will lower the temperature of the material and ensure the longest possible working life when mixed.

# No thinner is required for the G-2216 Epoxy Non-Skid. The consistency as received is correct for rolling, spraying, brushing or trowelling applications.

# Some settling of grit may occur in kits that have been in storage for a considerable length of time. This condition can be improved by turning cans of base material upside down 24 hours prior to mixing and by ensuring, during the mixing operation, that grit is loosened by scraping the bottom of the can.

# Add the small can of accelerator to each I gallon or 5 gallon container of base material.

# Mix thoroughly using power mixer. Scrape sides and bottom of container to ensure complete mixing. Approximately 10 to 15 minutes of mixing will be required.

PHYSICAL PROPERTIES

G-2216 DURADECK

Heavy-duty epoxy non-skid coating

Binder Type:	Epoxy-Polyamide

Pigmentation:	Titanium Dioxide, Aluminum Oxide, Silica

Mixing Ratio:	Base: 100 parts by weight

Activator: 5.3 parts by weight

Specific Gravity:	Mixed paint: 1.6 kg/l	14.5lb/gal.

Consistency:	Thixotropic liquid containing aggregate

Volume Solids:	48 +/- 2

Drying Time		Touch	18 hours

Hard	96 hours

Recoat	Min. 36 hours; Max. None

Flash Point		80o F Closed cup

Color	          Black, Dark Gray, Light Gray, Yellow, Red, Green, White, Olive    Drab. Others available upon request

Stability at 20o C	Shelf life 1 year

Pot life 4 hours

Storage at 68o F	Store in cool dry conditions

Temperature		Application 50o - 90o F

Finish:			Textured

G-501, G-501-Ml-7 Epoxy Non-Skid

GENERAL DESCRIPTION

G-501 Epoxy Non-Skid is a lightweight, non-slip deck covering compound developed for use on aluminum, steel, wood, concrete or polyester. This two-part system meets all the requirements of MIL-D-23003 (Ships) Type H. It is designed for use over Gryphin’s G-249 Primer and G-250 Primer. G-501 Epoxy Non-Skid contains a synthetic resinous binder and abrasive particles. It is easy to apply, economical to use, durable, and has the following advantages:

## It produces a deck covering which is tough with extremely long-wearing characteristics and which maintains excellent adhesion to the deck surface.

## The coating is resistant to fire and jet blasts and is odorless and sanitary. It has an excellent appearance and is resistant to extreme temperature changes.

## It is resistant to oil, greases, jet fuels, salt water and most acids.

G-501 Epoxy Non-Skid has a shelf life in excess of one year when stored in tightly sealed containers. It has been applied on many naval and commercial vessels with outstanding success.

G-501 Epoxy Non-Skid is available in I gallon and 5 gallon two-component kits. Each kit is supplied with the proper proportions of base material and accelerator. The entire kit should be mixed at one time; any attempt to mix less than the entire kit may result in an incorrect proportion of accelerator to base material, which will result in improper curing.

G-501-MI-7 formulation is the same as the formulation for G-501 except G-501-MI-7 contains a lighter, static-eliminating ingredient. On a volume basis, G-501-MI-7 coating is half the weight of a G-501 coating. All the information in this Bulletin applies equally to each formulation.

SURFACE PREPARATION

In order to obtain optimum adhesion to a surface, that surface must be free of all foreign matter. Any dirt, grease, oil, rust or other matter will prevent maximum available adhesion and will somewhat reduce the life of the Non-Skid coating. For best results sandblast to a white metal surface. The procedure to be followed in surface preparation is as follows:

## Clear the area to be cleaned of all loose equipment and rolling stock.

## Rope of area of convenient size for cleaning and priming.

## Post "Keep Off" and "No Smoking" signs.

## For metal surfaces:

## a. Clean the area with a Tenant Machine followed by sanding with disc   or drum sander

## b. Remove all dust with dry oil-free compressed air

## c. Coat the surface with Gryphin G-249 or G-250 Primer

## 5. 	For concrete surfaces:

## a. Sandblast with dry, grease-free sand.

b. If sandblasting is not possible, clean with Tenant Machine followed by disc sander, drum sander and wire brushes.

## c. Remove all dust with dry oil-free compressed air.

## d. Coat the surface with Gryphin G-249 or G-250 Primer.

6. For more detailed instructions see Gryphin Bulletin on Surface Preparation.

MIXING INSTRUCTIONS

G-501 Epoxy Non-Skid is a two-part deck covering compound. The two parts must be thoroughly mixed before use. The following procedure is recommended:

## If G-501 Epoxy Non-Skid is stored in the sun, it is recommended it be placed under cover for 24 hours before mixing. This will lower the temperature of the material and ensure the longest possible working life when mixed.

## No thinner is required for the G-501 Epoxy Non-Skid. The consistency as received is correct for rolling, spraying, brushing or trowelling applications.

## Some settling of grit may occur in kits that have been in storage for a considerable length of time. This condition can be improved by turning cans of base material upside down 24 hours prior to mixing and by ensuring during the mixing operation that grit is loosened by scraping the bottom of the can.

## Add the small can of accelerator to each I gallon or 5 gallon container of base material

## Mix thoroughly using power mixer. Scrape sides and bottom of container to ensure complete mixing. Approximately 10 to 15 minutes of mixing will be required.

METHOD OF APPLICATION

For roller applications, an excellent surface profile may be obtained with a Frieze No. 6 roller or a core type roller.

Gryphin G-501 Non-Skid may also be applied with spray equipment, using a bottom feed With 3/ 4 " hose, I/ 4 " fluid nozzle, and I/ 4 " airtip.

CURING TIME

Temperature 	Curing Time

70o F 		24 hours

50o F 		72 hours

APPLICATION TEMPERATURE LIMITATIONS

When surface and air temperatures are above 70o F, G-501 Series Non-Skids and Gryphin Primers will cure at a faster rate than shown above. When surface and air temperatures are below 50o F, external heat is required to cure the Non-Skids. Under these conditions it is recommended that the supplier be contacted for technical assistance. It should be remembered, however, that with air temperatures below 50oF, a deck under hot sun might develop deck surface temperatures approaching 80oF.

HUMIDITY AND DEWPOINT (NAVSEA CHAP. 634)

Humidity has a substantial impact on surface preparation and on how well the coatings cure. The 85% maximum relative humidity requirement is the accepted standard. When the 85% limit is exceeded, the metal substrate, before being primed, corrodes much faster than if the relative humidity were lower. Also, when the maximum limit is surpassed, the cure of most paints is slowed and sometimes altered. 'Me result can be blooming or blushing followed by the failure of the coating systems. The dew point is also critical during surface preparation and the application of coatings. The dew point is the temperature at which water will condense on a surface at a given humidity. In order to avoid moisture contamination and corrosion failure, the substrate temperature should be 5' above the dewpoint temperature.

CLEAN-UP

Equipment used for the application of G-501 Non-Skid Coating can be cleaned up with xylene or Methyl Ethyl Ketone. Avoid skin contact; refer to cautionary section of this brochure.

AVAILABLE COLORS

Gryphin G-501 Non-Skid is available in:

- Black

- light gray

- dark gray

- yellow

- red

- green

- white.

THICKNESS AND COVERAGE

When applied by roller at an average of 20 mils film thickness, each gallon will cover approximately 50 sq. ft. When applied by spray, at an average film thickness of 15 mils, each gallon will cover approximately 55 sq. ft.

WORKING LIFE (Pot Life)

Working life is the time during which the mixed G-501 Epoxy Non-Skid can remain in the container at a specified temperature and still remain usable. This may vary with volume of material and temperature. The following table gives the working life of quantities up to 5 gallons at three different temperatures.

Temperature		Working Life

70o F			8 hours

100o F			5 hours

If the lid of the container is left off for a prolonged period of time, there will be a loss of solvent resulting in an increase in viscosity of the material. This should be avoided.

## G-1191 	One-Part Water-Based Non-Skid Coating

GENERAL DESCRIPTION

G-1191 Non-Skid is a lightweight, non-slip floor and deck covering compound developed for use over aluminum, steel, wood, concrete or polyester. This material is used on areas subject to foot traffic in confined spaces. It is long wearing with a hard, non-porous surface and is resistant to extreme temperatures.

G-1191 Non-Skid contains a synthetic, resinous binder and abrasive particles. Because it is water-based, it is easy to apply, especially in areas where solvents are a problem.

SURFACE PREPARATION

In order to obtain optimum adhesion to a surface, that surface must be free of all foreign matter. This one-part water- based system can be applied directly over prepared concrete or over G-249 of G-250 primer when applied over wood, steel, aluminum or polyester. For best results, please review the Gryphin Surface Preparation Manual.

METHOD OF APPLICATION

An excellent surface profile may be obtained with a brush or short-nap roller. Gryphin G- 1191 Non-Skid may also be applied with spray equipment, using an agitated bottom feed pot with 3/4" hose, 1/4"'fluid nozzle, and 1/4" airtip.

CURING TIME

At 70o F 24 hours (foot traffic).

AVAILABLE COLORS

Gryphin G- 1 191 Non-Skid is available:

- black

- light gray

- dark gray

- yellow, red

- green, and white

Arrangements can be made for other colors

THICKNESS AND COVERAGE

When applied by roller or brush at an aver-age of 20 mils film thickness, each gallon will cover approximately 50 square feet. When applied by spray at an average film thickness of 15 mils each gallon will cover approximately 55 square feet.

CLEAN-UP

Because G- 1191 Non-Skid is water-based, equipment used for application can be cleaned with water.

GRYPHIN DURADECK NON-SKID COATING SERIES

Coefficient of Friction Characteristics

Due to its high coefficient of friction under wet or oily conditions, Duradeck provides an excellent non-skid surface for all types of flooring. The coefficient of friction values shown in the following bar graphs were obtained with an Olsen Medical Products Horizontal Pull Slipmeter, and assumes the use of rubber-soled safety shoes. Surface conditions that gave a coefficient of friction of less than 0.50 are considered slippery. The bar graphs demonstrate the vast superiority of Duradeck over other types of floor surfaces.

GRYPHIN DURADECK NON-SKID COATING SERIES

Wear resistance Characteristics

Wear Resistance

Wear in inches after I 00 revolutions on wear test machine

Wear tests conducted on a Tinius Olsen Tester greatly accelerates wear encountered under normal usage. This graph indicates the exceptional wear characteristics of each of the Duradeck formulations after 100 revolutions on the wear test machines. Least wear is encountered by G-2216 which experienced wear of only .010" after being subjected to the accelerated test. G-501 has sufficient wear resistance to give excellent service for most application.

CAUTION

Contains combustible solvent. Use with adequate ventilation. Keep out of reach of children. Do not breathe vapors. Solely for industrial and commercial use. Avoid skin contact during application; may cause minor skin or eye irritation.

EYE CONTACT: Wash/Flush immediately with low pressure flowing water for at least 15 minutes. Be sure entire eye is flushed. Get medical attention at once.

SKIN CONTACT: Remove contaminated clothing at once. Use disposable wipes to take liquid off the skin before cleaning. Clean skin immediately with soap and water. Do not use shop solvents to clean the skin. If there is any sign of redness, itching, or a burning. Get medical attention. Launder clothing before reuse. If material is accidentally swallowed, get medical attention immediately.

NOTE:

The information contained in this brochure is believed to be reliable and accurate; however, the Gryphin Co. cannot guarantee results or accept responsibility for operations not subject to their direct control.